PRODUCT DATA

FORMULA 2985

ALKALINE BOIL OUT COMPOUND

DESCRIPTION AND USE

FORMULA 2985 is a highly concentrated mixture of alkaline cleaners and detergents, chelating agents and scale/embrittlement inhibitors designed specifically for the pre-operational cleaning of industrial boilers and certain other water systems.  The product is formulated to remove both organic and inorganic deposits and to precondition the exposed metal surfaces to minimize flash rusting prior to startup of the program subsequently applied.  The product is not effective for hardness scale (calcium carbonate, etc.) removal which generally requires an acid medium.  It is effective for typical mill scale and the light oils and greases found on new equipment and in equipment which has been contaminated by hydrocarbon leaks.

APPLICATION AND TREATMENT REQUIREMENTS

FORMULA 2985 is normally applied at the rate of 1 to 2 gallons/100 gallons contained in the boiler for the boil out procedure.  The product is usually pumped into the boiler through one of the vents while the unit is being filled with water.  The manufacturer's procedure for boil out should then be followed.  If this is not available, use the instructions on the Technical Data sheet "Cleaning of Boilers for Oil and Grease Removal."  For use in the cleaning of other equipment, follow the instructions provided by the Technical Service Representative servicing the facility.

TYPICAL PROPERTIES

Appearance	Clear, colorless liquid

Odor	Characteristic

Flash Point	None

Specific gravity	1.240 - 1.250

pH (undiluted)	> 13.5

Freeze Point	< 0ºC (32ºF)

SAFETY AND HANDLING

FORMULA 2985 may be toxic by ingestion and because of its high causticity, is corrosive to human tissues.  Do not take internally.  If ingested, drink at least two (2) glasses of water and GET IMMEDIATE MEDICAL ATTENTION.  Do NOT induce vomiting.  Contact with eyes causes severe irritation or burns.  If eyes are contacted, immediately flush with clear water for 15 minutes and get medical attention.  For skin contact, wash with soap and water.  For additional information, see the Material Safety Data Sheet provided with this product.

PACKAGING

FORMULA 2985 is packaged in 55, 30, and 15 gallon, non-returnable plastic drums and 5 gallon, non-returnable pails.