PRODUCT DATA

FORMULA 2162-F

BOILER WATER TREATMENT

DESCRIPTION AND USE

FORMULA 2162-F is a concentrated blend of alkalinity builders and sodium sulfite with a combination of carboxylated organic polymers.  The product is designed for use in boiler systems having unsoftened makeup and a feedwater temperature of >150oF or a low alkalinity softened makeup with a feedwater temperature of >180oF.  For some systems, no other treatment chemicals will be required to complete the program.

FORMULA 2162-F is specifically formulated to comply with FDA regulations published in CFR - 21 part 173.310 entitled "Boiler Water Additives".  It is USDA registered for use in boilers where steam contacts food or edible products.

CHEMICAL FEEDING AND CONTROL

FORMULA 2162-F is normally fed continuously to the system being treated.  However, shot feeding may be satisfactory in some circumstances.  The product may be fed neat but is most often mixed in a chemical feed tank with the other materials required to complete the program.  Normal materials of construction are satisfactory for the feed system.  However, copper, copper alloys and aluminum must be avoided.

FORMULA 2162-F is controlled by an alkalinity test on the boiler water.  The specific control ranges vary depending upon system operating conditions and will be specified by the technical representative servicing the facility.

TYPICAL PROPERTIES

Appearance	Dark brown to light brown liquid

Odor	None

Flash Point	None

Specific Gravity (@ 22°C)	1.076 - 1.086

pH (undiluted)	13.0 - 13.5

Freeze Point	< -5ºC (23ºF)

SAFETY AND HANDLING

FORMULA 2162-F may be toxic by ingestion.  Do not take internally.  If ingested, drink at least two (2) glasses of water and get medical attention. Do NOT induce vomiting.  Contact with eyes causes severe irritation or burns.  If eyes are contacted, immediately flush with clear water for 15 minutes and get medical attention.  For skin contact, wash with soap and water.  For additional information, see the Material Safety Data Sheet provided with this product.

PACKAGING

FORMULA 2162-F is packaged in 55, 30, and 15 gallon, non returnable plastic drums and 5 or 6 gallon non-returnable plastic pails.